Quality description of European oak 								09.09.14

- Quality requirements of Class 1:

- Healthy knots till 10 mm allowed on one side allowed. The other side the knots can be 20 mm.

No dead knots allowed.

- Sapwood: maximum 25 mm on each side allowed (see pictures).

| Option 1: | Option 2: | Option 3: |
| --- | --- | --- |

- No full center allowed (see pictures)

- One center strip of 50 cm long on one side of the board allowed (see pictures)

| © Full center is not allowed. | (d) Center stripes of 50 cm are allowed. |
| --- | --- |

- Quality decription of  39 and 51 mm thickness,  European oak (3 qualities)

- ¾ sides defect free, no center, no center stripes, 10 mm sapwood on on one  sides (so one side knots are allowed)

- Mix-quality:
-  maximum knot size is 70 mm
-  maximum knot size of dead knots is 20 mm
-  cracks smaller than 100 mm
-  sapwood < 25 mm per side
- no yellow discolouration, insect attacks and bark/wane allowd
- No Center stripes allowed!
- No Center allowed!!!

| © Full center is not allowed. | (d) No center stripes allowed. |
| --- | --- |

- Rustical-quality:

- center allowed, at max 30 % of the boards

- center stripes allowed

- big knots allowed

- one dimension per parcel.

- sapwood < 25 mm per side

- Quality decription of 26 mm mix-quality,  European oak

-  core, center stripes of 1/3 length of the board allowed on 15 % of the boards!
-  maximum knot size is 70 mm
-  maximum knot size of dead knots is 20 mm
-  cracks smaller than 100 mm
-  sapwood < 25 mm per side, max on 20 % of the boards